SECTION 092900 - Gypsum Board, USG Securock® Brand Glass-Mat Sheathing Firecode® X

Product Summary:

- 1/2" Regular and 5/8" Type X glass-mat sheathing panels with moisture and mold resistance. - Direct substitute for USG Sheetrock® Brand Gypsum Sheathing (Regular and Firecode® X) when prolonged weather exposure is anticipated. - Coated fiberglass on both faces to maximize coverage of air/water barrier systems. - Treated gypsum core, combined with fiberglass face and back, offers exceptional water resistance. - Meet or exceed the requirements of ASTM C1177. - UL Classification as to fire resistance, surface-burning characteristics and noncombustibility. - Guaranteed for five years against manufacturing defects and have a 12-month limited-exposure warranty. - Comprehensive product and system testing assures long-term performance and safety. - Achieved GREENGUARD Gold Certification. - Refer to product submittal sheet WB2452 for more information.

Note to Specifiers:

- This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections: 09 29 00 – GYPSUM BOARD. - Areas where moisture and mold resistance is desired - Areas where glass-mat panels are desired. - Use in most exterior systems when properly detailed by exterior finish manufacturer. - Under exterior claddings where conventional gypsum sheathing products have traditionally been used, such as brick veneer, properly detailed Exterior Insulation Finish Systems (EIFS), clapboard siding, panel siding, shingle siding, shake siding and conventional stucco. - USG Securock® Brand Glass-Mat Sheathing Firecode® X can be used for any UL design where UL Type USGX panels are listed

- 2.2   SHEATHING PANEL, GLASS MAT EXTERIOR GYPSUM BOARD, USG SECUROCK®                    BRAND GLASS-MAT SHEATHING FIRECODE® X

        - Gypsum Board ASTM C 1177 “Standard Specification for Glass Mat Gypsum Sheathing”: Type X.

          - Basis of Design: Subject to compliance with project requirements, the design is based on the following: “USG Securock® Brand Glass-Mat Sheathing Firecode® X”.

          - UL Type Designation “USGX”.

          - ASTM D 3273: Mold Resistance:

            - Score of 10 as rated according to ASTM D 3273.

          - Thickness: [1/2” (12.4)] [5/8” (15.9)].

          - Length: [8’-0” (2438)] [9’-0” (2743)] [10’-0” (3048)] [12’-0” (3658)].

          - Widths: 48" (1219).

          - Weight: [2.0] [2.7] lb./ft2.

          - Long Edges: Square.

          - Bending Radius: 8’-0” (2438).

Disclaimer:  The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project.  These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.