SECTION 092900 - USG Sheetrock® Brand Abuse Resistant Firecode® X Panels

|  |
| --- |
| **Sustainability Notes:** |
| * Achieved GREENGUARD Gold Certification. |

|  |
| --- |
| **Product Summary:** |
| * Designed and tested to offer greater resistance to surface indentation and impact damage than standard USG Sheetrock® Brand Gypsum Panels * Meets ASTM C1629 Level 1 for soft- and hard-body impact and indentation resistance * Underwriters Laboratories Inc. (UL) Classification as to fire resistance, surface burning characteristics and noncombustibility * Refer to product submittal sheet WB2133 for more information. |

|  |
| --- |
| **Note to Specifiers:** |
| * This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections:   09 29 00 – GYPSUM BOARD.   * Maximum framing spacing for walls is 16" o.c. * Avoid exposure to excessive, repetitive or continuous moisture before, during and after installation. Eliminate sources of moisture immediately. * Must be stored off the ground and under cover in accordance with Gypsum Association publication GA-801, Handling and Storage of Gypsum Panel Products. * For abuse-resistant construction over steel framing, minimum 20-gauge drywall steel studs (0.0312" design thickness) as defined by the Steel Stud Manufacturers Association (SSMA) are required. * Not suitable for use as a substrate for tile in wet areas such as tubs and showers, gang showers and other areas subject to direct water exposure. |

1. ABUSE AND MOLD RESISTANT INTERIOR GYPSUM BOARD
   * + - 1. Abuse Resistant Gypsum Board ASTM C1629: Standard Classification for Abuse-Resistant Non-decorated Interior Gypsum Panel Products and Fiber-Reinforced Cement Panels.

Basis of Design: Subject to compliance with project requirements, the design is based on the following: “USG Corporation, Sheetrock® Brand Abuse Resistant Firecode® X Panels”.

Abrasion Resistance; Level 2.

Indentation Resistance; Level 1.

Soft Body Impact Resistance; Level 1.

Hard Body Impact Resistance; Level 1.

UL Type Designation “AR”.

Thickness: 5/8 inch.

Length: [8’-0” (2438)] [9’-0” (2743)] [10’-0” (3048)] [12’-0” (3658)].

Widths: 48" (1219).

Weight: 2.8 lb./ft2.

Long Edges: Tapered.

Disclaimer: The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project. These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.