SECTION 09 29 00 – GYPSUM BOARD, 5/8 in. (15.9 mm) USG Sheetrock® Brand EcoSmart Panels Firecode 30® (UL Type FC30)

|  |
| --- |
| **Sustainability Notes:** (Architecture 2030 Challenge for Products – LEED® v4 EPD/LCA improvements) |
| * USG Sheetrock® Brand EcoSmart Panels Firecode 30® (UL Type FC30) are formulated and manufactured using the most sustainable method to date
	+ Up to 25% less global warming potential (GWP)1
	+ Up to 30% less weight reduces transportation fuel energy by up to 20%
	+ Living Building Challenge™ Red List Free
	+ Contain 100% USDA certified biobased content
	+ Up to 97.3% recycled content (regionally available)
	+ Achieved GREENGUARD Gold Certification and qualify as a low VOC emitting material (meets CA 01350)
	+ USGBC® LEED® v4 **–** may assist in achieving additional credits
* Developed to meet the Architecture 2030 Challenge for Products, USG Sheetrock® Brand EcoSmart Panels Firecode 30® (UL Type FC30) have lower carbon dioxide emissions than standard Type X gypsum board. These values are defined by the Gypsum Association’s Type III EPD per ISO 14040 for North American gypsum board.

|  |  |
| --- | --- |
| **Gypsum Panel** | **CO2 eq. (kg CO2/1000 sq. ft.)** |
| **USG Sheetrock® Brand EcoSmart Panels Firecode 30®** **(per EPD 218)** | **207** |
| GA Industry Average **–** Standard 5/8 in. (15.9 mm) Type X  | 277 |

1. Compared to standard 5/8 in. (15.9 mm) Type X gypsum panels as presented in the Gypsum Association’s *5/8 in. (15.9 mm) Type X Conventional Gypsum Board Environmental Product Declaration* (EPD 10270). |

|  |
| --- |
| **Product Summary:**  |
| * Sustainable and ultralightweight 5/8 in. (15.9 mm) panels for interior wall and ceiling applications
* Feature an innovative noncombustible gypsum core encased in 100% recycled face and back papers that form a high strength-to-weight ratio composite design
* Comply with ASTM C1396, *Standard Specification for Gypsum Board*, for 5/8 in. (15.9 mm) and non-Type X gypsum wallboard
* Underwriters Laboratories Inc. (UL) Classification as to fire resistance (30-minute and 1-hour fire-rated walls), surface-burning characteristics and noncombustibility
* Offer comparable strength and sag resistance to standard 5/8 in. (15.9 mm) Type X
* Can be used in any UL Design in which Type FC30 panels are listed
* For more information, refer to product submittal sheet WB2858 or usg.com
 |

|  |
| --- |
| **Note to Specification Writers:** |
| * This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections: 09 29 00 – GYPSUM BOARD.
* This product is manufactured at USG gypsum panel plants, reducing distances and carbon footprint for transport.
* Panels shall be installed in accordance with GA-216, *Specifications for the Application and Finishing of Gypsum Panel Products* and ASTM C840, *Standard Specification for Application and Finishing of Gypsum Board*.
* Contact USG at800.874.4968 for technical questions.
 |

PART 2 – GYPSUM PANEL PRODUCTS

* + - 1. SUSTAINABLE NON-TYPE X GYPSUM PANEL
				1. ASTM C1396, *Standard Specification for Gypsum Board*, for 5/8 in. (15.9 mm) and non-Type X gypsum wallboard

Basis of Design: Subject to compliance with project requirements, the design is based on the following: United States Gypsum Company, USG Sheetrock® Brand EcoSmart Panels Firecode 30®

ISO 14040 Environmental Management, Life Cycle Assessment, Principles and Framework:

Carbon emissions per Gypsum Association; Industry Standard Type III EPD
for North American Type X wallboard have a Global Warming Potential value
of 277 CO2 eq.: **207 kg CO2/1000 sq. ft.**

Primary energy from non-renewable resources per Gypsum Association; Industry Standard Type III EPD for North American Type X wallboard have a value of 4,100 MJ/1000 sq. ft.: **3,730 MJ/1000 sq. ft.**

UL Type Designation: “FC30”

ASTM E136 Noncombustibility: Meets

ASTM E84 Surface-Burning Characteristics

Flame Spread: 15

Smoke Developed: 0

Class A (Flame spread not greater than 25 and smoke developed not greater than 450): Meets

ASTM C473, *Standard Test Methods for Physical Testing of Gypsum Panel Products*

Core Hardness

Field [Not less than 11 lbf (49 N)]: Meets

End [Not less than 11 lbf (49 N)]: Meets

Edge [Not less than 11 lbf (49 N)]: Meets

Flexural Strength

Parallel [Not less than 46 lbf (205 N)]: Meets

Perpendicular [Not less than 147 lbf (654 N)]: Meets

Nail Pull Resistance [Not less than 87 lbf (387 N)]: Meets

Humidified Deflection [Not greater than 5/8 in. (15.9 mm)]: Meets

Thickness: 5/8 in. (15.9 mm)

Length: 8-16 ft. (2438-4877 mm)

Width: 4 ft. (1219 mm)

Weight: 1.7 lb./sq. ft. (8.3 kg/sq. m.)

Edge: Tapered

Shear Value for Wood-Frame; Screws, 8 in. (203 mm) OC perimeter, 12 in. (305 mm) OC field: 75 plf

Shear Value for Wood-Frame; Nails, 4 in. (102 mm) OC perimeter, 7 in. (178 mm) OC field: 127 plf

Disclaimer: The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project. These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.