SECTION 09 29 00 – GYPSUM BOARD, 1/2 in. (12.7 mm) USG Sheetrock® Brand Firecode® C Panels (UL Type C)

|  |
| --- |
| **Product Summary:** |
| * 1/2 in. (12.7 mm) enhanced proprietary Type X panels for interior wall and ceiling applications
* Feature a noncombustible gypsum core that is encased in 100% recycled face and back papers that form a high strength composite design
* Comply with ASTM C1396, *Standard Specification for Gypsum Board*, for 1/2 in. (12.7 mm) and Type X gypsum wallboard
* Underwriters Laboratories Inc. (UL) Classification as to fire resistance, surface-burning characteristics and noncombustibility
* Can be used in any UL Design in which Type C panels are listed
* Achieved GREENGUARD Gold Certification and qualifies as a low VOC emitting material (meets CA 01350)
* For more information, refer to product submittal sheet WB2965 or usg.com
 |

|  |
| --- |
| **Note to Specification Writers:** |
| * This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections: 09 29 00 – GYPSUM BOARD.
* This product is manufactured at USG gypsum panel plants, reducing distances and carbon footprint for transport.
* Panels shall be installed in accordance with GA-216, *Specifications for the Application and Finishing of Gypsum Panel Products* and ASTM C840, *Standard Specification for Application and Finishing of Gypsum Board*.
* Contact USG at800.874.4968 for technical questions.
 |

PART 2 – GYPSUM PANEL PRODUCTS

* + - 1. TYPE X GYPSUM PANEL
				1. ASTM C1396, *Standard Specification for Gypsum Board*, for 1/2 in. (12.7 mm) and Type X gypsum wallboard

Basis of Design: Subject to compliance with project requirements, the design is based on the following: United States Gypsum Company, USG Sheetrock® Brand Firecode® C Panels

UL Type Designation: “C”

ASTM E136 Noncombustibility: Meets

ASTM E84 Surface-Burning Characteristics

Flame Spread: 15

Smoke Developed: 0

Class A (Flame spread not greater than 25 and smoke developed not greater than 450): Meets

ASTM C473, *Standard Test Methods for Physical Testing of Gypsum Panel Products*

Core Hardness

Field: [Not less than 11 lbf (49 N)]: Meets

End: [Not less than 11 lbf (49 N)]: Meets

Edge: [Not less than 11 lbf (49 N)]: Meets

Flexural Strength

Parallel: [Not less than 36 lbf (160 N)]: Meets

Perpendicular: [Not less than 107 lbf (476 N)]: Meets

Nail Pull Resistance: [Not less than 77 lbf (343 N)]: Meets

Humidified Deflection: [Not greater than 1-1/4 in. (32 mm)]: Meets

Thickness: 1/2 in. (12.7 mm)

Length: 8-12 ft. (2438-3658 mm)

Width: 4 ft. (1219 mm), 54 in. (1372 mm)

Weight: 2.0 lb./sq. ft. (9.8 kg/sq. m.)

Edge: Tapered

Disclaimer: The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project. These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.